## Slide 1: W and D-Band – State of Technology Tudor Williams – Director of Technology Andy Tucker – Engineering Manager

## Slide 2: Summary
Wireless X-Haul
Why W and D-Band?
Move to W-Band
  Product Form and Fit
  Semiconductor Availability
  Manufacturing Challenges
  Roadmap for W-Band
Technology Challenges at D-Band
  Product Form and Fit
  Semiconductors
  Work to Date - Manufacturing Challenges
Conclusions

## Slide 3: Wireless X-Haul
* Ericson Microwave Outlook October 2021
Continued Importance of Wireless X-Haul –
Wireless backhaul still more than 50% share of the market in 2026 in many regions.
Decrease in share countered by more hops to support demand.
Continued increase in bandwidth demand across urban, sub urban and rural.
Higher mmWave links fundamental to future networks.
* Ericson Microwave Outlook October 2020

## Slide 4: Why W and D-Band?
5G and Beyond –
With the roll out of 5G we have seen increased adoption of higher mmWave bands such as E-band to deal with the increased backhaul of data. As we move to 6G and beyond we expect to see use-cases requiring extreme performance, with extreme data rates.
W-Band, due to band assignment will offer similar channel bandwidth and performance as E-band (10Gb/s), simpler deployment
D-band has the potential to support extreme data rates up to 100GB/s with 4x25GB/s MIMO, supporting extreme bandwidths for future applications.

## Slide 5: W-Band

## Slide 6: W-Band Product Form factor
Integrated Transceiver
Use as an extension of E-band, plan to use same form factor, allows re-use of investment at E-band with possibility to leverage existing modems
Maximum 2GHz channel size
Can maintain similar link lengths to E-band
Accelerated deployment due to small shift in required architecture
W-Band | 
Sub Band (GHz) | Net Bandwidth
92-94 | 3.5
94.1 – 100 | 5.5
102 -109.5 | 7.25
111.8 – 114.25 | 2

## Slide 7: W-Band Semiconductor Availability
Very limited commercially available MMIC’s (particularly Power amplifiers) available in W-band.
Leading GaAs pHEMT open foundry offerings beginning to seriously address W-Band with their 0.1um node processes, expect to see further improvements in the coming 12 months further increases to gain and power density.

## Slide 8: Manufacturing Challenges
Incremental but not without challenge.
Push towards more integration of chipset, reduce number of interconnects to reduce loss in transitions.
Increased placement tolerances, compatible with our current wire-bond/pick and place.
Increased tolerances for manufacture of waveguide diplexer – from current ±5um to ± 2um (possible but expensive)

## Slide 9: Filtronic W-Band Roadmap
Preliminary MMIC’s
Full
MMIC’s
Integrated
MMIC’S
Fab 1
W-Band Chipset
Milestones
Diplexer W-Band
Tx/Rx W-Band
SiP Development
M1
Active Diplexer
Initial SiP Dev (Cyane)
SiP for W-Band
M3
Feb 2022
March 2025
Full Transceiver Development
M4
M2
M5
Fab 2
Fab 3
 | Milestone Detail
M1 | Improved MMIC PA for E-Band product lines
M2 | W-Band Active diplexer Demonstrator
M3 | W-Band device demonstrators
M4 | Q/V band design simulations
M5 | W-Band Chipset Available
M6 | W-Band Transceiver product
3 year timeline fits with expectation of the market
E Band
W Band

## Slide 10: D-Band

## Slide 11: D-Band Product Form factor
Chip Scale packaging approach
* From www.3DinCites.com
Form factor for D-Band will be very different, likely we will see a shift towards even greater levels of integration mixing base-band with high frequency using technologies such as SiGe
Still require a Power amplifier and LNA for point to point links, interposer will be critical to accommodate multiple. semiconductor technologies.
Complex assembly issues in terms of precision of placement and interconnects.
Possible move from frequency to spatial multiplexing due to narrow beam width.

## Slide 12: D-Band Semiconductor Availability
No commercially available MMIC’s available at present.
GaAs power processes do not have sufficient gain or power density to support power amplifier devices, expect to see lower node size of 0.07um to address D-band market appearing in 12-18 months.
Parallel work required to co-design parts for volume manufacturing.

## Slide 13: Work to Date at D-Band

## Slide 14: Manufacturing Challenges – Interconnects and transitions at D-Band
A major constraint at D-band is interconnects between MMICs and transitions from microstrip to waveguide.
While ribbon bonding is still relatively low loss at E-band but is no longer viable at D-band.
New assembly methods required, four methods investigated in this work, two looking at microstrip to waveguide transitions and two methods considering MMIC to MMIC connections.

## Slide 15: MMIC to MMIC Interconnect – Design
Bumps
Quartz substrate
Thru connection
Feed Line
Quartz substrate
GSG Pads

## Slide 16: MMIC to MMIC Interconnect – Experimental Results
Overall loss of the structure is between 0.43 and 1.2 dB between 140-170 GHz
Feed line structures are de-embedded using a TRL calibration kit manufactured on the same wafer
Good agreement between measurement and simulation
Transition loss of between 0.43 and 1.08 dB over 140-175 GHz

## Slide 17: MMIC to WG Transition – Design
WR5 Connection
Capacitive Post
Resonant Cavity
1.6mm Line
Waveguide Probe
AMC Pin array
Waveguide Feeds & mmic carrier
Lid with AMC array
Assembled Split block test fixture
Patterned backside Metal

## Slide 18: MMIC to WG Transition – Experimental Results
Overall loss of the structure is between 1.4 and 2.0 dB between 140-170 GHz
Measurements are de-embedded using s-parameter measurements of waveguide thru and on wafer microstrip line
Very good agreement between measured and simulated performance
Transition loss of between 0.32 and 0.62dB over 140-175 GHz

## Slide 19: Conclusions
Increasing requirements on data rate for telecoms X-haul leads to requirements for higher frequency bands to deal with additional demand.
W-band will be adopted first as an adjacent band to E-band, allows leverage of existing technology and assembly methods. Allows for simple integration into the Network for fast roll-out.
D-Band allows for improved data rates that will be required for future telecoms, particularly in dense urban environments
More challenges to solve at D-band including underlying semiconductor technology and assembly/integration for volume production.